## Slide 1: Pen-on-Paper Flexible Electronics
Analisa Russo
In collaboration with Jennifer Lewis
and Bok Yeop Ahn
Notes: Add Illinois and MRL logos

## Slide 2
Demo
Instructions: draw whatever you want on the card – just don’t short out the LED!

## Slide 3
Paper-based electronics
High porosity
Energy storage materials
High flexibility
Foldable thermochromic displays
Biodegradable
Disposable RFID tags
Inexpensive
Paper-based microfluidics
A.C. Siegel, et. al, Adv. Funct. Mater. 2010, 20, 28.
L. Hu, et. al, PNAS 2009, 106, 21490.
V. Lakafosis, et. al, Proc. IEEE. 2010, 98, 1601.
A. C. Siegel, et. al, Lab on a Chip. 2009, 9, 2775.

## Slide 4
Ink-based manufacturing
Large-scale additive fabrication:
Small-scale fabrication and prototyping:
Screen printing
Gravure and roll-to-roll
Inkjet printing
Direct Ink Writing (DIW)
B.Y. Ahn, E.B. Duoss, Science. 323 (2009).
Notes: What is missing from the toolbox? You probably noticed that paper is portable, lightweight, ubiquitous – but none of these techniques are.

## Slide 5
Rollerball pen writing of microelectrodes
Like paper, the rollerball pen is lightweight, portable, inexpensive.
It can be used to create devices “on-the-fly…”
…it is also an intuitive design tool
Notes: What’s missing? A tool that is as ubiquitous and inexepnsive and portable as the paper substrate itself. What we found, after using the pen for some time, is that it is also an intuitive design tool.

## Slide 6
4 mm
1 mm
4 mm
Rollerball pen writing of microelectrodes
Ruler
Stencil
Spirograph
Regular drafting tools can be used to create uniform shapes
Notes: For example, regular drafting tools can be used to create uniform shapes, without the need for setting up equpiment or writing a program.
As an aside – these are some magnetic components that we borrowed from Leah buechely’s group at the media lab: I’ll talk about these again later…

## Slide 7
Large pigment particles: creates bold colors that are visible on dark paper
Shear thinning ink: flows through tip without leaking or skipping, enables suspension of large particles
Rollerball pen ink: an advanced material
Commercial ink
Our ink
Notes: Our inspiration for ink design came from commercial rollerball pens – already a highly engineered fluid.
Compare to something we know: 10 Pa-s = melted chocolate, 0.1 Pa-s is

## Slide 8
Conductive ink for rollerball pen
drying
Ink is composed of water and a cellulose binder – replace large pigment particles with conductive silver…
…upon drying, the particles form a continuous conductive network.
Notes: Has all of the target design parameters to commercial rollerball ink, in addition to requiring high conductivity

## Slide 9
Ink synthesis
50 ml water
40 ml diethanolamine
1.95 g poly (acrylic acid)
20 g silver nitrate
20 hours
5 hours

## Slide 10
Ink synthesis
Grow particles to 400 nm diameter

## Slide 11
Ink synthesis
Transfer to larger beaker
Coagulate particles with ethanol

## Slide 12
Ink synthesis
Centrifuge at 9000 rpm to collect particles
before
after

## Slide 13
Ink synthesis
Filter ink through 10 micron pore filter
Add viscosifier:
Hydroxyethyl cellulose
HEC:Ag = 3:100 by weight

## Slide 14
shear rate = 1 s-1
clogging
leaking
Tuning ink viscosity
Simply change water content to adjust viscosity
A viscosity “writing window” exists where ink flows through tip without leaking or clogging
A. Russo, B.Y. Ahn, et. al, Adv. Mater. 2011

## Slide 15
Printed ink microstructure and resistivity
bulk silver
100°C
50oC, 2 hr
250°C
2 μm
Low resistivity after writing
Cellulose burns out
Particle sintering
Notes: Resistivity is a material property that describes how well it an conduct electrons – can be measured directly.

## Slide 16
LED kit
Bending apparatus
Robotic stage
d = 40 mm
d = 35 mm
d = 30 mm
d = 20 mm
d = 10 mm
d = 0 mm
Flexible printed microelectrodes on paper
Radius of curvature = 5mm

## Slide 17
Flexible printed microelectrodes on paper
1.5 cm printed electrodes are bent repeatedly to three difrerent radii of curvature (slight bend, to almost creased)
Resistance is measured after when paper is in a flat orientation
A crease develops in paper after 10,000 bend cycles
A cold joint is formed in the flat state, restoring conductivity
1 bend cycle
10,000 cycles
A. Russo, B.Y. Ahn, et. al, submitted to Adv. Mater. 2011
Notes: Conductive trace fails when the paper fails!

## Slide 18
Applications

## Slide 19
Electronic art
1 cm
50 m
500 m
2 um
Paper substrate
Conformal silver ink
LED attachment
Notes: Famous korean painting Sae han do. One of our post-docs traced this. Good illustration of how this ink works. Surface mount LED attached with conductive epoxy

## Slide 20
Surface mount LED array, drawn by hand and dried at room temperature
(2516) 400 LEDs, operated by a 9 V battery
4 mm
1 mm
4 mm
LED display

## Slide 21
A. Russo, B.Y. Ahn, et. al, Adv. Mater. 2011
Radio frequency antenna

## Slide 22
LED display
Applications of pen-on-paper electronics
Conductive touch-pad
3D antenna
Electronic art
Notes: Surface mount LED array, drawn by hand and dried at room temperature
(2516) 400 LEDs, operated by a 9 V battery

## Slide 23
Pen-on-paper for education:
Girls Learning about Materials “GLAM” summer camp

## Slide 24
Resistors in series and in parallel

## Slide 25
LED project

## Slide 26
Fab Lab workshop
Champaign-Urbana community

## Slide 27
Teardrop project, MIT:
Magnetic components
Throwies:
Our version:
Laser cut acrylic pads, press fit magnets and through-hole components

## Slide 28
Practical circuits

## Slide 29
Magnetic components 2.0
through-hole components
Laser-cut masonite
Press-fit magnets
Triangle-shaped LED component indicates diode direction
Notes: Fab lab workshop was a nerdy crowd, so their feedback was to make the components look more like the symbols

## Slide 30
Capacitive sensors and programmable devices
Magnets used to hook up devices to an Arduino board

## Slide 31
Acknowledgements
Advisor: Jennifer A. Lewis
Collaborators: Bok Yeop Ahn, Brett Walker
Lewis Group Members
Funded by: DOE MRL
We believe that the P-o-P electronics is a versatile approach to prototyping devices and is a valuable teaching tool.
Goals:
Continue to improve the interface between P-o-P electronics and existing DIY tools like the Arduino system
Develop an expanded palette of materials that can be used for P-o-P electronics (ionic conductors, insulators, magnetic inks)
Conclusions